CORPORATE SPECIFICATION DOSSIER

LOW STRENGTH PROPPANT

ONGC/WS/27/2015  |  v0

| Document class | Controlled Technical Document |
| --- | --- |
| Category | Well Stimulation Chemicals |
| Specification status | Current / Published |
| Corporate register | Yes |
| Prepared by | Dinesh Reddy_106228 |
| Reviewed by | — |
| Last revised | 21 Aug 2026 |
| Generated | 22 Aug 2026, 04:50 IST |

Purpose: This dossier consolidates the current corporate specification, covered register chemicals, technical requirements, material information, impact controls and version history into one read-only review and reference document.

Generated from the live ONGC Digital Workspace record. Uncontrolled when printed.

# 1. Executive Summary

LOW STRENGTH PROPPANT is maintained under ONGC/WS/27/2015. This controlled release contains 22 specification parameters and covers 3 corporate-register chemical entries.

| PARAMETERS | VERSION | IMPACT | REGISTER |
| --- | --- | --- | --- |
| 22 | v0 | LOW IMPACT | Yes |

## Document Control

| Specification | ONGC/WS/27/2015 |
| --- | --- |
| Chemical | LOW STRENGTH PROPPANT |
| Version | v0 |
| Test procedure | ONGC/ Test Procedure Vol-III / WS / 27 |
| Material reference | 090001039 (LSP 12/20) |
| Standard testing time | 1 day |
| Prepared by | Dinesh Reddy_106228 |
| Reviewed by | — |

## Covered Register Chemicals

| S. No. | Chemical / Grade | Material Code | Testing Time |
| --- | --- | --- | --- |
| 1 | Low Strength Proppant (12/20) | 90001039 | 1 day |
| 2 | Low Strength Proppant (20/40) | 100101589 | — |
| 3 | Low Strength Proppant (40/70) | 100000281 | — |

# 2. Specification Requirements

The following requirements constitute the current controlled parameter set. Parameter classifications are shown below each parameter name.

| S. No. | Parameter | Required Value | Unit | Method / Conditions |
| --- | --- | --- | --- | --- |
| 1 | Physical State Essential | The material shall be in the form of single grains | — | — |
| 2 | Sieve Analysis: Size Designation LSP 12/20 Essential | ASTM No. 12 / 20 or equivalent | — | — |
| 3 | Sieve Analysis: Size Designation LSP 20/40 Essential | ASTM No. 20 / 40 or equivalent | — | — |
| 4 | Sieve Analysis: Size Designation LSP 40/70 Essential | ASTM No. 40 / 70 or equivalent | — | — |
| 5 | Fraction retained between the designated sieves sizes, percent by mass Essential | 90.0 (Minimum) | — | — |
| 6 | LSP 12/20: Fraction retained on ASTM No. 8 or equivalent sieve, percent by mass Essential | 0.1 (Maximum) | — | — |
| 7 | LSP 20/40: Fraction retained on ASTM No. 16 or equivalent sieve, percent by mass Essential | 0.1 (Maximum) | — | — |

| S. No. | Parameter | Required Value | Unit | Method / Conditions |
| --- | --- | --- | --- | --- |
| 8 | LSP 40/70: Fraction retained on ASTM No. 30 or equivalent sieve, percent by mass Essential | 0.1 (Maximum) | — | — |
| 9 | LSP 12/20: Fraction passing through ASTM No. 30 or equivalent sieve, percent by mass Essential | 1.0 (Maximum) | — | — |
| 10 | LSP 20/40: Fraction passing through ASTM No. 50 or equivalent sieve, percent by mass Essential | 1.0 (Maximum) | — | — |
| 11 | LSP 40/70: Fraction passing through ASTM No. 100 or equivalent sieve, percent by mass Essential | 1.0 (Maximum) | — | — |
| 12 | Sand Grain Clusters, percent by count Essential | < 1 | — | — |
| 13 | Krumbein Sphericity Essential | 0.6 (Minimum) | — | — |
| 14 | Krumbein Roundness Essential | 0.6 (Minimum) | — | — |
| 15 | LSP 12/20: Acid solubility in 12% (w/w) HCl + 3% (w/w) HF on dry basis, percent by mass Essential | 2.0 (Maximum) | — | — |

| S. No. | Parameter | Required Value | Unit | Method / Conditions |
| --- | --- | --- | --- | --- |
| 16 | LSP 20/40: Acid solubility in 12% (w/w) HCl + 3% (w/w) HF on dry basis, percent by mass Essential | 2.0 (Maximum) | — | — |
| 17 | LSP 40/70: Acid solubility in 12% (w/w) HCl + 3% (w/w) HF on dry basis, percent by mass Essential | 3.0 (Maximum) | — | — |
| 18 | Turbidity on dry basis, NTU Essential | 250 (Maximum) | — | — |
| 19 | LSP 12/20: Crush resistance at 3000 psi fines, percent by mass Essential | 16 (Maximum) | — | — |
| 20 | LSP 20/40: Crush resistance at 4000 psi fines, percent by mass Essential | 14 (Maximum) | — | — |
| 21 | LSP 40/70: Crush resistance at 5000 psi fines, percent by mass Essential | 8 (Maximum) | — | — |
| 22 | Clay and soft particle content, percent by volume Essential | 1 (Maximum) | — | — |

# 3. Specification Narrative

## Background

Version 0 : Legacy 2015 Specification

## Recommendation

Migration to 2026 version with type classification of all parameters into Vital and Desirable

# 4. Material and Handling Profile

## Material Identity

| Material Code | 090001039 |
| --- | --- |
| Material Short Text | LOW STRENGTH PROPPANT |

## Storage and Handling

| Storage Conditions - General | Store in a cool, dry, well-ventilated place away from moisture, heat, and direct sunlight |
| --- | --- |

# 5. Impact and Issue Controls

## Impact Summary

| Impact Classification | LOW IMPACT (Provisional) |
| --- | --- |
| Decision Rule | No triggers found — 10 flag(s) still at REVIEW |
| Red YES Count | 0/5 |
| Amber YES Count | 0/5 |
| Flags Answered | 0/10 |

## Assessment Flags

| Assessment Dimension | Recorded Response |
| --- | --- |
| HSE / Hazard | REVIEW |
| Op-Acute | REVIEW |
| Op-Chronic | REVIEW |
| Safety-critical | REVIEW |
| Environmental-critical | REVIEW |
| Environment | REVIEW |
| Regulatory | REVIEW |
| Supply Chain | REVIEW |
| Seasonal | REVIEW |
| Financial | REVIEW |

## Issue Register

| Issue Domain | Status | Recorded Note |
| --- | --- | --- |
| Operational | NO ISSUE RECORDED | — |
| Quality | NO ISSUE RECORDED | — |
| Supply | NO ISSUE RECORDED | — |
| Testing | NO ISSUE RECORDED | — |

# 6. Governance and Revision Record

| Version | Date | Action | Recorded By | Reason / Note |
| --- | --- | --- | --- | --- |
| v0 | 10 Mar 2026 | Reset Baseline | Dinesh Reddy_106228 | Version history reset; current content preserved as v0 |

## Review Note

Version history reset; current content preserved as v0